#### APPROVAL  SHEET

承 认 书

客    户      ：

产品型号      ：       EE28-HT-P4

规    格      :  平面  AL=3600±25%nH/N2

日    期      ：       2017/4/27

客户认可： APPROVAL BY (为确保订单顺利，请在1个月内认可或回复) 如有客户品码(料号)，请填写在下 客户品码(料号)：

承认书    APPROVAL  SHEET

| 认可标准SPECIFICAION FOR APPROVAL: 产品型号P/N: EE28-HT-P4 材料特性 单位 HT-P4 初始磁导率ui(10KHZ) 25℃ 2400±25% 饱和磁通密度Bs(H=1194A/m) 25℃ mT 510 100℃ mT 390 剩磁Br 25℃ mT 100 100℃ 55 矫顽力Hc 25℃ A/m 14 100℃ A/m 9 电阻率ρ Ω.m 5 居里温度Tc ℃ ≥220 功率损耗 25℃ mW/cm3 710 100℃ mW/cm3 410 |
| --- |
| Item: FERRITE CORE | P/N: EE28-HT-P4 | SPEC./N: |

承认书    APPROVAL  SHEET

| 1.产品型号P/N: EE28-HT-P4 2.材质Material: HT-P4 3.电磁性能Electromagnetic property: 3.1测试项目及测试条件Test Item & Condition: 项目1 Item1: 电感系数Inductor Value: 测试条件 Test Condition: *测试仪器Testing Instrument: LCR2810 *测试频率Test Frequency: 1KHZ *测试电压Test Voltage: 0.3V *测试温度Test Temperature: 25±3℃ *测试圈数Test Turns: 100TS 3.2电感系数Inductor Value: AL=3600±25%nH/N2 3.3功率损耗Power Loss： 100KHZ 200mT 100℃ Pcv<130mW /g |
| --- |
| Item: FERRITE CORE | P/N: EE28-HT-P4 | SPEC./N: |

承认书    APPROVAL  SHEET

| 4.尺寸 Dimensions:(mm) |
| --- |
| A: 28.5±0.4 B: 10.5±0.3 C: 10.5±0.3 D: 7.2±0.3 Emin:19.0 F: 6.3±0.3 |
| Item: FERRITE CORE | P/N: EE28-HT-P4 | SPEC./N: |

承认书    APPROVAL  SHEET

| 5．外观质量：Outside Quality： a.磁芯表面应无明显氧化，铁锈，油渍,及裂缝. 磁芯表面清洁，无肉眼可见疏松铁氧体或其它附着物。 There are no crack and oxide in the ground surface of core. b.磁芯表面上掉块面总面积不超过2.0mm2,数量不多于三处。 The total chip square should be no more than 2.0 mm2and quantity should be no than 3. 6.检验方法（Inspection Method）： 按GB2828-87，一次正常抽样，检查水平II，AQL符合下列标准。 According to GB2828-87, one time normal random sampling,Inspect level II，AQL should be as follows； AQL Inspcect Item A 0.65 Electromagnetic Property B 1.0 Outside Size C 1.5 Outside Quality 7.包装Packing: 内包装:泡塑；外包装采用纸箱,每箱产品外面都贴上产品合格证（包括型号、规格、材质、数量、批号、检验员）和环保标签。 Inside packing TBD，paper box is used to outside packing，Quality Certification is attached on every box，including Item（Product name or type），Quantity，Lot No.and Tester. |
| --- |
| tem: FERRITE CORE | P/N: EE28-HT-P4 | SPEC./N: |